## Slide 1
Fit for recycling – How inks enable a Circular Economy
German Paint and Printing Ink Associations
Represented by Ewald Rempel (Sun Chemical) & Alina Marm (Siegwerk)

## Slide 2: What we want….
Recycling of plastic waste with the least loss of material value  high quality recyclates
Foto credits: Siegwerk, https://www.awg-info.de/privatkunden/gelber-sack

## Slide 3: What we get…
Quality impairment of PCR1
Caused by contaminants like food residues, adhesives, barrier materials, inks, etc.
Odor
Gel particles, black spots
Mechanical properties
Discoloration
Color fluctuations
Optical uniformity
Haze
Washing
Extrusion > 200°C
PCR
Sorted input stream PCW
Recyclates that are not fit for broad use
1. Qualitative assessment, depending on the target application
Source: Recycling of flexible packaging - heat stable inks and deinking I Dec 2022
Notes: Props: shredded & extruded pellets, blown film (non-de-inked)

## Slide 4: Circular Economy and Recycling – a fast moving topic
Understand behaviour of today’s packaging structure on today’s recycling practices and improve it (Design for recycling – D4R)
Innovate inks and other packaging materials to support today’s recycling techniques
Innovate recycling techniques to improve recyclate quality. (Collecting/ Sorting/Deinking)
Today’s recycling techniques and packaging materials are not fit for the ambitious recycling goals on global, EU and national level Scientific background is often lacking (but improving)
How to get there?
EU Plastic packaging recycling rates/targets |  |  | 
2016 | 2021 | 2025 | 2030
42% | 40% | 50% | 55%
By 2030 all plastic packaging should be recyclable! |  |  | 
Huber – check source

## Slide 5: Let us explore how inks can contribute to the CE and recycling ambitions
The Life Circle Assessment perspective of inks in packaging
Supporting the move to monomaterials
Quo Vadis Nitrocellulose?
De-inking for high quality recyclate
Driving forces of a circular economy

## Slide 6
Circular Economy
Life Cycle Assessment

## Slide 7: What is Life Cycle Assessment?
  Life Cycle Assessment (LCA) is a systematic method for evaluating the environmental impacts of a product, process, or activity throughout its entire life cycle
  LCA considers various environmental aspects, such as resource depletion, energy consumption, greenhouse gas emissions, and other pollutants
  LCA helps identify areas where improvements can be made to minimize environmental harm and optimize sustainability - but is often lacking (but improving)

## Slide 8: Life Cycle Assessment (LCA) vs. Product specific assessment
Two different options to determine the environmental impact of a product
Life Cycle Assessment (LCA)
Must cover the full life cycle of a product
Printing inks are not manufactured for direct use by end customer
Product use phase & end of life are mainly unknown for printing ink manufacturer
Product specific assessment
Focussing only on the steps in the life cycle related to the ink manufacturing (direct impact)
Enable customers to calculate their own product related environmental impact
“Cradle-to-gate” approach
1. Raw Material manufacturing
2. Product manufacturing
3. Transport
4. Product Use Phase
5. End of Life
3. Transport
4. Product Use Phase
5. End of Life
1. Raw Material manufacturing
2. Product manufacturing
Notes: Purpose Emphasize the difference on LCA and how cradle-to-gate is just a fraction of the full life cycle. Why cradle-to-gate etc.?

## Slide 9: Cradle-to-gate approach
In Scope
Raw Material Production
End of Life
Customer Gate
Ink manufacturer’s Gate
Use phase
Cradle-to-grave
Cradle-to-gate
Enables the printing ink manufacturer to control the environmental impact of stages in its own hand
  Raw material supply (supplier firsthand data retrieval possible)
  Own manufacturing process
Enables customer to calculate their own environmental impact
No double counting along the value chain
Reflecting the ink manufacturing impact in the best possible way
Notes: Purpose: Explain difference boundaries, explain why we have these systems. Notes: Key point; avoid double counting, check your boundaries: Quickly explain the term “cradle” “end of life” etc.

## Slide 10: Printing Ink manufactures in the value chain
Printing ink producers are only a small piece of the long value chain
Only ~2% of the finished product carbon footprint is the ink contribution
Position: Middle of first half of the value chain
The position of a printing ink manufacturer in the value chain is directly impacting the contribution of an ink to the footprint of the final product
Example: Value chain for packaging of filled goods
Use phase
end-customer
End of life
Selling product on the market
Filling product in packaging
Filling good production
Packaging printing
Printing Ink production
Substrate production
Additive production
Resin production
Pigment production
Solvent production
Raw material production
Packaging end production
Packaging components (e.g., glue) production
Notes: Purpose: Explain value chain and how our position influences our ability to do calculations.

## Slide 11
Circular Economy
Supporting the move to mono-materials

## Slide 12: Why use Flexible Packaging structures?
Price competitiveness
Eye-Catcher - presentation of the product - advertisement
Less weight and waste volume compared to glass or metal containers
Barrier functions protecting the product light, moisture, oxygen, microbial activity, taste & smell, evaporation, physical containment

## Slide 13: Complexity of packaging structures versus recycling
Multimaterial packaging has lately become under pressure due to the combination of various materials with different properties like polymers, aluminum and inorganic barrier coatings
Multimaterial packaging is therefore difficult to recycle in existing waste management infrastructures without a de-lamination step before de-inking and granulation
A reduction of material complexity would most likely cause a shorter shelf-life, especially of food products
The trend points towards monomaterial structures based on Polyolefin substrates in combination with suitable barrier coatings like SiOx and AlOx which are fully compatible in the recycling stream

## Slide 14: Typical Flexible Packaging Components
Monomaterials
Organic coating
Ceramic coating
Metallization
Multilayers
Thin layer coating of metallic aluminum
Combination of various monomaterials and barrier coatings
Acrylics
EVOH
PVdC
Silicon Oxide (SiOx)
Aluminium Oxide (AlOx)
Polyolefins (PE & PP)
Polyester (PET)
Polyamide (PA)

## Slide 15: Barrier Properties of Packaging structures

## Slide 16: Monomaterials
Advantages
Disadvantages
Typical substrates: PE, PP, PET and PA
Poor gas barrier though properties are increasing with polymer density PE  PA
PET and PA not compatible with Polyolefin recycling stream
Easy to recycle (after de-inking)
No need for de-lamination
Good moisture barrier
Flexible

## Slide 17: Coated Polyolefins
Advantages
Disadvantages
Typical substrates: BoPP coated with Acrylic, EVOH or PVdC
Problematic for recycling – reduces quality of the recyclate (yellowing)
PVdC may release carcinogenic dioxines when heated during extrusion of recyclate
Very high moisture barrier
Very high O2 barrier
Good aroma barrier
Crack resistant
Acrylic coated layer
Transparent OPP core layer
Acrylic coated layer
Enhanced Low Seal PVdC Coating
Oriented Polypropylene
Enhanced Low Seal PVdC Coating

## Slide 18: Ceramic coating
Advantages
Disadvantages
Typical substrates: PET, BoPP, PA
Not crack resistant (glass like) – potential loss of barrier properties
AlOx can be challenging to overprint
SiOx can be difficult to laminate
Cost
Generally, very high all-round barrier properties
Fully compatible in recycling stream
Not detected by metal detectors
Suitable for microwave
Corona Treatment
AlOx Coating
Protect Layer
Plain Surface
PET Core Layer

## Slide 19: Metallization
Advantages
Disadvantages
Typical substrates: PET, BoPP
Not separable during recycling causing discolouration of recyclate
Detected by metal detectors
Not suitable for microwave
Generally, very high all-round barrier properties
Light barrier
Improved optical aspects
BOPP Core Layer
Corona Treatment
Metalized Layer
Heat-Sealing Layer

## Slide 20: Multilayers
Advantages
Disadvantages
Typical substrates: Combination of different materials and barrier coatings
Not fully recyclable without prior de-lamination into monomaterials
Need for de-lamination primer
Generally, very high all-round barrier properties
Tailored design for very specific needs
Protection of barrier coatings
Structural
Printed
Outer
Adhesive
Inner/Seal
Barrier
Adhesive
Multilayer Flexible Packaging
Printing ink

## Slide 21: Quo Vadis Nitrocellulose?
Practical solutions in a changing market environment
NEXT STEP
FUTURE

## Slide 22: What is nitrocellulose?
Nitrocellulose (NC) is a common binder system used in solvent-based printing inks and varnishes for Flexible Packaging to a very large extend
In flexo and gravure printing this technology covers approximately more than 80% of the entire market for solvent-based inks in Europe
X
Y
n
X + Y =1

## Slide 23: Printing inks for Flexible Packaging
NC = nitrocellulose PU = polyurethane PVC = polyvinlyl chloride PVB = polyvinyl butyral
J
J
K
L
universal
very high
J
L
J
J
L
Binders account for around 10-20% of a solvent-based ink
NC is a very versatile binder system with many pros but also a very strong con ...
Typical binder systems and their properties – pros and cons
Binder
NC, NC/PU
PVB
PVC
PU
Gravure printability
Flexo printability
Pasteurisation
Sterilisation
Range of substrates (adhesion)
Printing speed
Surface printing
Lamination High Perfromance
Lamination Medium perfromence
Lamination Standard Performance
Mechanical recycling
J
K
J
J
universal
high
L
J
J
J
J
J
L
J
J
universal
very high
L
J
J
J
L
J
J
J
J
very universal
very high
L
J
J
J
J

## Slide 24: The future of NC inks
Regranulation 240 – 250°C
Printed Film Polymers
Mechanical re- cycling (thermal process)
Physical Recycling
Volatiles, filter residue
Sorting and Cold washing
Physical recycling is a thermal process that leads to thermal decomposition of temperature sensitive nitrocellulose
Physical Recycling

## Slide 25: The future of NC inks
Current ink binders flexible packaging
Flexo printing:
90% Nitrocellulose (NC)
Gravure printing:
75% NC 25% PVB, PVC and PU for high temperature (sterilization 120–130°C) applications
Upcoming / new regulations
German “Minimum Standard” Large format PE laminates printed with NC are not compatible with German recycling system; but: no legal or financial consequences
Packaging & Packaging Waste Regulation (EU) By 2030 all packaging must be recyclable – non-recyclable packaging will be banned Criteria will be defined (“delegated acts”)
Design for recycling (D4R) criteria by European Standard (CEN Institute) Anticipated for 2027
Ceflex and RecyClass D4R guideline amendment expected for Q4 2023/ Q1 2024 based on ongoing scientific evaluations
vs
Check and rephrase

## Slide 26: The future of NC inks
Good news: There are potential alternatives available
Alternative binders (PU, PVB)
Modified mechanical recycling process: Deinking instead of “only” cold-washing
Conclusion
We will get some kind of specific D4R criteria for inks (‘Mindeststandard’, RecyClass, Ceflex, CEN, PPWR) in the future
Criteria and details to need to be defined

## Slide 27
De-inking for creating high quality recyclates

## Slide 28: PU-ink systems are better suited for mechanical recycling, but it is not a silver bullet
PE reference
Nitrocellulose, white
Polyurethane, white
Nitrocellulose, CMYK (std. pigments)
Polyurethane, CMYK (HPP)
Optical appearance of extruded film based on printed material
Qualitative overview impact binder
Property | General purpose NC-ink | Heat-stable PU-ink
Gassing during extrusion | Not ok | Ok
Odor recyclate | Not ok | Ok
Gel particles, mechanical properties | Not ok | Not ok – Ok
Discoloration recyclate | Not ok | Not ok
Suitable for food contact (FCM) | No | No
Source: Recycling of flexible packaging - heat stable inks and deinking I Jul 2023

## Slide 29: De-inkable solutions allow production of colorless recyclates from printed Post Consumer Waste (PCW)
1. No additives / masterbatch, 100% recyclate content in films
Source: Recycling of flexible packaging - heat stable inks and deinking I Jul 2023
Basic steps de-inking
Material input
Flaking of
printed film
Washing of
film flakes
Regranulation of de-inked material
Use of granulate for new product
De-inkable solutions and chemistry
With de-inking
W/o de-inking
Not De-inked
De-inked1

## Slide 30: Making packaging de-inkable
Source: Recycling of flexible packaging - heat stable inks and deinking I Jul 202
Systematic de-inking studies of all relevant print structures on-going
De-inking of any structure possible, but can require too harsh conditions for cost-efficient industrial application (time, temperature, chemicals)
1K SB inks proven to be optimal for de-inking
De-inking primers allow for de-inking of most inks
De-inking primers can delaminate, extending the range of de-inking possibilities
De-inking resistance
Suitability for alkaline hot-wash de-inking
2K coatings
UV- / EB-inks and coatings
2K solvent-based inks
1K solvent-based inks
Offset (oil-based)
With
Primer

## Slide 31: Delamination/de-inking primers ensure smooth de-inking of reverse-printed structures
Option 2
Source: Recycling of flexible packaging - heat stable inks and de-inking I Jul 2023
De-inkable structure with Primer
Delamination/de-inking of OPP/met-OPP structure
OPP
Colour Ink
White Ink
Adhesive
Metallized OPP
Primer
Notes: The next deinking product is addressing another flexible packaging recycling pain point – which are laminated structures.
As laminated structures are normally reverse-printed, the ink is sandwiched between 2 films and not easily removable from the substrate. Therefore, we have developed a series of alkali strippable primers that facilitate both the opening of the laminate structure and removal of the ink in a hot caustic washing step.
Note that the final performance can depend on the type of adhesive used. In many cases, efficient deinking requires a second breaking point in the structure, due to adhesive initiated cross-linking of the ink. The 2nd breaking point could be a metallization layer, as demonstrated on the schematic, a barrier coating or another layer of the DDP on top of the white. In any case, this is currently not a plug-and-play product and testing is required.
WB-system -> CirKit ClearPrime WB A04 (SAP Code 15-607789-3) -> good performance, but not accepted by converters printing solvent-based systems due to low printing speed and exhaust issues. Previous testing has shown inconsistent BSVs.
SB-system -> CirKit ClearPrime DP 6300 (SAP Code 10-616061-7) -> still undergoing optimization for reaching industrial printing speeds.

## Slide 32: De-inking/de-laminatio can be combined with printed coatings for barrier
Printed oxygen barrier
Oxygen barrier coating
Color / White
PE
Primer
Delamination / de-inking primer
MDO-PE
Adhesive
Enabled by functional coatings
Stand-up pouch with high barrier
Flakes after de-inking
Notes: For delamination deinking to take place, the primer must be either combined with a WB-adhesive, or a second breaking layer must be introduced, e.g., metallization or as in this case the OBC, that also dissolves under alkaline conditions releasing the ink from the adhesive.

## Slide 33: De-inking is emerging in the market, but needs application at scale
1: Link to CEFELX: CEFLEX ‘Quality Recycling Process’ - CEFLEX2: Link to Coveris PR: Coveris opens new ReCover recycling facility with pioneering technology | Coveris; 3: Huthamaki Annual Report, 2022, p. 165; 4: Siegwerk
Industry initiatives
Packaging converters
De-inkable on market / ready for market4
CEFLEX Quality Recycling Process (QRP)1
Coveris – UK (PE films)
ReCover recycling facility2
Huthamaki – Turkey3

## Slide 34
Driving forces of a circular economy

## Slide 35: Key Success Factors
Circular Design
Produce & Manufacture
Consume
Collect, Sort & Recycle

## Slide 36: Circular Design
Increasing (harmonized) design for recycling guidelines
From multi-material to mono-material
Reduce unnecessary packaging
Inks, primers and OPVs have a key role in Circular Design: barrier, heat-stable inks, de-inking etc.
Circular Design
Produce & Manufacture
Consume
Collect, Sort & Recycle

## Slide 37: Produce & Manufacture
Increase the use of recycled material (food contact suitable)
Replacing fossil raw material with bio-renewable alternatives
Optimize production: reduction of waste
Investment in transition to monomaterial packaging structures
Circular Design
Produce & Manufacture
Consume
Collect, Sort & Recycle

## Slide 38: Consume
Circular Design
Produce & Manufacture
Consume
Collect, Sort & Recycle
Consumers are paying more attention to the problem of plastic waste
Do not forget about reusable options
Goal: Consumer acceptance of recycled packaging

## Slide 39: Collect, Sort & Recycle
Circular Design
Produce & Manufacture
Consume
Collect, Sort & Recycle
Recycling conserves dwindling resources
Extended Producer Responsibility Laws
Recycling needs investments (e.g. de-inking, sorting technologies)
Support: Waste separation at household level

## Slide 40: Circular Economy and Recycling – a fast moving topic
Activities on regulatory level
Packaging and Packaging Waste Regulation
CEN Working group - Design for recycling for plastic packaging products
Global regulatory trends
Activities on Industry level
CEFLEX
RecyClass
APR
Market movement

## Slide 41: Quo Vadis Circular Economy?
What will tomorrow’s recycling techniques look like (chemical recycling)?
Which packaging structures can be economically recycled?
Do you see different adoption speed of circular packaging globally (e.g. is Europe faster than Asia or North America)? Which region is leading?
How do you see the future pf plastic. Or do you see the trend going towards paper?

## Slide 42: Thank you!
Feedback welcome
Q&A

## Slide 43
www.WirSindFarbe.de